氧化铁红系列
	型号
	简介

	110
	Bright,600 mesh Easy to stir and disperse strong covering power 

	130
	Universal 

	190
	Used in coatings,electronics, construction,rubber and plastic industries,color stability！ 



Technical indicator
	Fe2O3
	≥95%
	pH value
	6.0-7.0

	water soluble matter
	0.4%
	Relative coloring power
	95-105%

	Sieve residue
	0.3%
	Oil absorption
	20ml/100g

	105℃volatile matter
	0.8%
	heat resistance temperature
	≥500℃



氧化铁黄系列
Yellow iron oxide has excellent tinting power,hiding power,alkali resistance and acid resistance.
It is widely used in building materials, papermaking, coatings,plastics,rubber products,artificial marble and other fields. 

	型号
	简介

	313
	Universal
For example,catalysis,papermaking industry 


	312
	Applicable to cement products, coatings,etc.
High cost performance 


	314
	适用于制动片、水泥制品、涂料等。色彩稳定、分散性高



Technical indicator
	Fe2O3
	85%
	pH value
	4.0-6.0

	water soluble
matter
	0.4%
	Relative coloring power
	95-105%

	Sieve residue
	0.3%
	Oil absorption
	30ml/100g

	105℃volatile
matter
	1.0%
	Particle size
	0.3-2μm

	Solubility
	Insoluble in water and alcohol,soluble in acid




氧化铁黑系列

特性：1、Bright blue black with high tinting strength 
2、 Outdoor weather resistance,long-lasting and non-fading 
3、 Fine powder, easy to disperse 


型号：720、710、炭黑、特黑，以下技术指标仅适用于710、720，不适用于炭黑和特黑

Technical indicator
	Fe3O4
	≥92%

	water soluble matter
	0.3%

	Sieve residue
	0.3%

	pH value
	5.0-8.0

	Relative coloring power
	95-105%

	Oil absorption
	12-25ml/100g

	density
	1.0g/m³









氧化铁蓝系列

型号：非洲蓝、群青、深蓝、酞青蓝、铁蓝

氧化铁绿系列
型号：835、5605、美术绿、酞青绿、铁绿。

氧化铁棕系列
型号：深棕、浅棕

氧化铁橙系列
型号：铁橙

氧化铁灰系列
型号：深灰、浅灰

二氧化钛系列
型号：S-1699 
Technical indicator
	Type
	Rutile

	TiO2 content
	95%

	Oil absorption
	13-15

	Screening residue
	≤0 .08

	Water soluble
	≤0 .3

	Moisture
	≤1.0

	pH
	7-8

	Chromatic Aberration
	≤1.0

	Application Areas
	Universal




铬黄系列
型号：浅铬黄、中铬黄、深铬黄、柠檬铬黄
Technical indicator
	型号
	铬酸铅含量
Lead chromate
content
	水溶物
Water
sol salts
	遮盖力
Covering
power
	着色力
Tinting
strength
	吸油量
   Oil obs
(ml/100g)
	筛余物
( 3 2 0 目 筛 )
meshres

	深铬黄
	≥85%
	≤1%
	≤45g/m²
	≥95%
	≤22%

	≤0.5%

	中铬黄
	≥90%
	≤1%
	≤55g/m²
	≥95%
	≤22%
	≤0.5%

	浅铬黄
	≥60%
	≤1%
	≤75g/m²
	≥95%
	≤30%
	≤0.5%

	柠檬铬黄
	≥50%
	≤1%
	≤95g/m²
	≥95%
	≤30%
	≤0.5%












氧化铬绿系列
型号：氧化铬绿
简介：用于涂料、陶瓷、橡胶、美术颜料、以及伪装涂料等
Technical indicator
	Cr2O3
	99%

	water soluble matter
	0.5%

	Moisture content
	0.3

	pH
	5-8

	Tinting Strength
	100±5

	Oil absorption
	≤16

	Screening residue
	0.05
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